Ukleid International MFG

The leather and Textile Garments Manufacturer & Exporter

Technical Leather Specification Sheet: Protective Motorcycle Gear

General Identification

Article:  Motorbike leather mild grain softy

Animal Origin: Cowhide for suits/jackets

Tannage Type: Chrome-Tanned

Finish Type: High performance Pigmented finish

Thickness Range: 1.1 mm – 1.3 mm (± 0.05 mm

- Surface Quality & Leather Grading:

Grade A   Minimum 85% clear cutting surface.

Mechanical & Performance Standards

Tear Strength 50 N (Double Edge Tear0 (ISO 3377-2 / EN 17092)

Tensile Strength   20 N/mm 9ISO 3376)

Abrasion Resistance 4.0 seconds (CE Level 2) (EN 13594 / EN 17092)

Flexing Endurance 100,000 dry cycles (ISO 5402-1)

Color Fastness to Rubbing Dry (100 cycles): Grade 4

Wet (50 cycles): Grade 3-4

Artificial Sweat (50 cycles): Grade 3-4 (ISO 11640)

Finish Adhesion 3.5 N/10mm (ISO 11644)

- Chemical Compliance (EU REACH Annex XVII)

Chromium VI < 3.0 mg/kg (ISO 17075-1)

Azodyes < 30 mg/kg (ISO 17234-1)

Free & Hydrolysed Formaldehyde: < 75 mg/kg (ISO 17226-1)

Pentachlorophenol (PCP) & Tetra chlorophenols (TeCP): < 0.5 mg/kg (ISO 17070)

Alkylphenols & Alkylphenol Ethoxylates (APEO/NPEO): < 100 mg/kg (ISO 18254-1)

Per- and Polyfluoroalkyl Substances (PFAS)

Substances of Very High Concern (SVHC): * *< 0.1% by weight