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Technical Leather Specification Sheet: Protective Motorcycle Gear
General Identification
Article:  Motorbike leather mild grain softy
Animal Origin: Cowhide for suits/jackets
Tannage Type: Chrome-Tanned 
Finish Type: High performance Pigmented finish
Thickness Range: 1.1 mm – 1.3 mm (± 0.05 mm
1. Surface Quality & Leather Grading:
Grade A   Minimum 85% clear cutting surface.
 Mechanical & Performance Standards
Tear Strength 50 N (Double Edge Tear0 (ISO 3377-2 / EN 17092) 
Tensile Strength   20 N/mm 9ISO 3376)
Abrasion Resistance 4.0 seconds (CE Level 2) (EN 13594 / EN 17092)
Flexing Endurance 100,000 dry cycles (ISO 5402-1)
Color Fastness to Rubbing Dry (100 cycles): Grade 4 
 Wet (50 cycles): Grade 3-4 
 Artificial Sweat (50 cycles): Grade 3-4 (ISO 11640)
Finish Adhesion 3.5 N/10mm (ISO 11644)




2.  Chemical Compliance (EU REACH Annex XVII)
Chromium VI < 3.0 mg/kg (ISO 17075-1)
 Azodyes < 30 mg/kg (ISO 17234-1)
 Free & Hydrolysed Formaldehyde: < 75 mg/kg (ISO 17226-1)
 Pentachlorophenol (PCP) & Tetra chlorophenols (TeCP): < 0.5 mg/kg (ISO 17070)
 Alkylphenols & Alkylphenol Ethoxylates (APEO/NPEO): < 100 mg/kg (ISO 18254-1)
 Per- and Polyfluoroalkyl Substances (PFAS)
Substances of Very High Concern (SVHC): * *< 0.1% by weight
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